## Slide 1: ECE 340 Lecture 23 Current Flow in P-N diode
Last time, we talked about unbiased P-N junction.
Today, biased (Vext ≠ 0) P-N junction and current flow.
Draw equilibrium (V = 0) bands:
Recall built-in voltage and depletion width:

## Slide 2
Qualitative band diagrams with applied voltage:
Current flow in equilibrium (V = 0):

## Slide 3
Qualitative current flow:

## Slide 4
Qualitatively expect I-V curve to be:
In forward bias, inside space charge region (SCR):
Where V is the applied bias and ___________________

## Slide 5
Let’s look at the injected minority carriers:
On the n-side, injected holes.
Just at the edge of n-side depletion region:

## Slide 6
Excess injected holes diffuse into the n-side:
(same is true of excess injected electrons on p-side).
Injected hole diffusion current:
Where equilibrium hole concentration pn0 =
(and similar for injected electron diffusion on p-side, just replace subscripts p with n)
Hole diffusion current proportional to excess hole concentration at any distance x into the n-type region.
Due to hole current continuity, we can evaluate at x=xn0=0

## Slide 7
We can also write diffusion current for electrons in p-side:
Now total current

## Slide 8: ECE 340 Lectures 24-26 P-N diode carrier injection; reverse bias & breakdown
Recap diode bias diagrams:
equilibrium
forward bias (V > 0)
reverse bias (V < 0)

## Slide 9
Recap some of the equations:
  Depletion width
  (decreases at forward bias, increases at reverse bias)
  Maximum electric field
  (decreases at forward bias, increases at reverse bias)
  Built-in voltage
  Charge stored

## Slide 10
  Current density (current I = J∙A)
  What about an asymmetrically doped junction? Say, p side much more heavily doped (NA >> ND):
Remember, current is due to minority carrier injection
Typically p-n junctions in real life are made by counterdoping. E.g. start with p-type wafer and dope with ND only at the surface to obtain junction. Eqs. so far readily apply if
  NA = net doping on p-side = (NA – ND)p-side
  ND = net doping on n-side = (ND – NA)n-side

## Slide 11
Ex: a p-n junction has NA=1019 cm-3 and ND=1016 cm-3. The applied voltage is 0.6 V. a) What are the minority carrier concentrations at the edges of the depletion region? b) What are the excess minority carrier concentrations? c) Sketch δn(x) on the p-side if recombination lifetime is 2 μs.

## Slide 12
Current continuity along junction length, JTOT = const.
As carriers recombine (deep into n- or p-side) the diffusion current is replaced by _____________
But, we were able to deduce current equation by simple diffusion arguments at the _________________ where the E-field was just barely zero.

## Slide 13
Reverse bias:
  Depletion region widens
  E-field across depletion region _________________
  Current is due only to minority carrier ______________ across the junction
  Current is supplied by EHP generation in the __________________ (what if I change the temperature or turn on the light?)
  Recall, J0 =

## Slide 14
Junction breakdown when E-field exceeds a critical value. If current continues increasing, then diode ______________ .

## Slide 15
P-N junction breakdown (3 types)
1) Zener breakdown:
  Dominant for heavily doped (>1018 cm-3) p+n+ diodes
  Breakdown at a few Volts (typically < 5 V)
  Electron tunneling from filled valence states on p-side into (mostly) empty conduction band states on n-side

## Slide 16
2) Avalanche breakdown
  More lightly doped junctions (<1017 cm-3)
  Wider depletion region, electrons accelerated across it gain enough energy to create additional EHPs
  Impact ionization and carrier multiplication

## Slide 17
Empirical observation of VBR with doping and material
  VBR decreases with increasing N (=NA or ND)
  VBR decreases with decreasing EG
Breakdown dependence on temperature:
  For tunneling (Zener) breakdown…
  For avalanche breakdown…

## Slide 18
3) Punchthrough breakdown:
  Occurs when either depletion region “punches through” the entire length of the diode, e.g. xn(V) = Ln
Ln