## Slide 1: ECE 340 Lecture 27 P-N diode capacitance
In reverse bias (V<0) fixed charge is stored in the junction, as the depletion width widens with more negative V.
Why? How does W change with voltage?

## Slide 2
If we measure and plot 1/CJ2 vs. V, I can get __________

## Slide 3
Ex: Diode with area 100x100 μm2, slope of (1/CJ)2 vs. V is -2x1023 F-2V-1, and intercept is 0.84 V. If NA >> ND, find the two sides’ doping.

## Slide 4
In forward bias (V>0) excess minority carriers are stored in the quasi-neutral regions of the p-n diode.
In n-side (note zero of x-axis redefined to xn0 = 0):
Where Δpn(xn) =
and Lp =
In p-side (note zero of x-axis redefined to xp0 = 0):

## Slide 5
Diffusion capacitance for holes in n-side:
Where ℓn = ________________
And pn = _________________
Keep in mind that in general CJ(V) = Cdepl + Cdiff
  “Long” diode = _______________________
  “Short” diode = _______________________

## Slide 6
We’ve (nearly) exhausted the p-n junction. Now we know:
  1) Why and how it conducts current (forward, reverse)
  2) How to calculate depletion width, field, built-in voltage
  3) How diodes break down
  4) How diodes store charge as capacitors
  5) How to make an LED or photodiode

## Slide 7
Two diode applications in optoelectronics:
Photodiode
or solar cell
2) Light-emitting diode (LED)

## Slide 8: ECE 340 Lecture 28-29 P-N optoelectronics; photodetectors, solar cells, LEDs
Recall: Si is great (cheap, good SiO2 insulator) for high complexity digital & cheap analog circuits
What if we want: High-speed (10s GHz – 1 THz) analog amplifiers; Optical receivers, emitters (LEDs, lasers)
Look at other semiconductors with BETTER mobility and light emission / absorption properties (“custom” EG).

## Slide 9
http://xkcd.com/273/

## Slide 10
Another thing to keep in mind:
  Direct band gap (EG) 
  Indirect band gap (EG) 
Ball-and-stick
lattice picture:
Band diagram picture:
Remember: EG = hf = hc/λ; numerically EG(eV) = 1.24/λ(μm)

## Slide 11
We now focus mostly on direct band gap semiconductors like GaAs, InP and their alloys:
Note, we can vary alloy
composition (e.g. InxGa1-xAs)
and get different _________
and _____________
Getting same lattice constant
as the substrate (GaAs or InP)
is important to minimize lattice
defects in a device.
Generally, assume lattice constant (a) and band gap (EG) vary linearly with alloy fraction (x)

## Slide 12
We know p-n junction can be used to:
  Emit light (EHP recombination at ___________ bias)
  Absorb light (EHP generation at ___________ bias)
Minority & majority carriers recombine and emit light
  In the ________________ region (WD)
  Within a _______________ length (Ln, Lp) in n- and p-sides

## Slide 13
Can we control & improve p-n light emission / absorption?
Use p-n heterojunction, i.e. make
depletion region in a material with
_____________ EG
Use p-i-n diode by making
depletion region intrinsic (“i”)
to enlarge depletion region W

## Slide 14
What are the current & voltage in an illuminated junction?
  1) Note: need illumination photon energy hf > EG
  2) Assume quantum efficiency Q.E. = 1 = one EHP created for every incoming photon
For example, if EHP generation is gop = 1017 EHPs/cm3/s
What is the optically generated current in a diode?

## Slide 15
How does the photogenerated current add (or subtract) to the current already induced by the diode voltage?
Short-circuit current: external V = 0  Isc = ____
Open-circuit voltage: external I = 0  Voc = ____
This is a photovoltaic effect.

## Slide 16
How fast is the photodiode speed (response frequency)?
fmax = …

## Slide 17
Ex: Photodiode Design. Consider a p-i-n photodiode (see Fig. 8-7), with “i” region made of InxGa1-xAs (see Fig. 1-13). Design stoichiometry “x” and thickness of the “i” region (Wi) to enable response at 1.3 μm wavelength, up to 20 GHz signals. Assume fields are sufficiently high to reach vsat ≈ 107 cm/s in the “i” region. Name at least one design constraint on the “p” and “n” regions of this photodiode. You may assume the lattice constant and band gap of InxGa1-xAs vary linearly with composition “x”.

## Slide 18
Optical fiber communications  why use wavelengths of 1.3 or 1.55 μm?
  Minimum _____________
  Minimum _____________

## Slide 19
Semiconductor lasers vs. LEDs:
  Strong fwd. bias, population inversion
  Recombination region + resonant cavity
  (length L, between semi-reflective mirrors)
  Stimulated emission at λ = 2L/m
resonant modes
between mirrors
in laser cavity

## Slide 20
http://www.infographicsshowcase.com/from-radio-receivers-to-led-flashlights-an-led-odyssey/coast-led-timeline/
(also see Fig. 8.10 in your textbook)