## Slide 1: ECE 340 Lecture 30 Metal-Semiconductor Contacts
Real semiconductor devices and ICs always contain metals. Why? _______________________
Metals are actually easier to treat than semiconductors:
  1) No band gap, only Fermi level matters
  2) ~100-1000x more electrons than highly doped silicon (no internal E-fields  flat energy bands in metals!)
Draw metal next to semiconductor,
define work function:

## Slide 2
Another scenario, if Φm < Φs
Contact potential V0
Use analogy to p+n
junction to evaluate
depletion width W:
Ex: calculate semiconductor work function qΦs if it is silicon doped p-type with NA=1017 cm-3

## Slide 3
Two types of metal-silicon contacts become apparent:
  1) Schottky (rectifying, like a diode)
  2) Ohmic
How do you get one vs. the other?
When would you want one vs. the other?
Silicon work function:
Some typical metal work functions:

## Slide 4
Schottky (rectifying) contact on n-type Si:
Apply V>0 on metal, reduce
built-in energy barrier.
  What happens?
  Can electrons flow from metal to Si?
Apply V<0 on metal, enhance built-in energy barrier.
qΦB =

## Slide 5
Ohmic contacts on silicon, two ways to achieve them:
  1) Choose metal with appropriate work function to “match” the Fermi level of p- or n-type Si
  2) Dope silicon highly, to thin out Schottky barrier, so electrons can tunnel through (almost) regardless of Φm

## Slide 6: ECE 340 Lecture 31-32 Metal-Oxide-Semiconductor (MOS) Capacitor
MOS capacitor, needed for MOSFETs and DRAM (and Flash):
  In nMOS device: n+ gate (or low Φm), p-substrate
  In pMOS device: p+ gate (or high Φm), n-substrate
Note gate = metal by Intel at 45nm tech node, since ~2008. Why?
SiO2 most common gate insulator (EG = 9 eV, εr = 3.9)
Intel switched to bilayer HfO2 (EG ≈ 5 eV, εr ≈ 20) with SiO2. Why?
d

## Slide 7
Metal/high-K MOSFET (we’ll come back to it later):
Draw band diagram of MOS capacitor with n+ gate and p-substrate.
source: intel.com

## Slide 8
We drew this as n+ gate MOS, but remember that gate can also be metal! Then metal gate work function Φm matters:
Define the bulk (body) potential:
Define the surface potential:

## Slide 9
What happens if we apply a gate voltage?
There are two important reference voltages here:
  1) Flat-band voltage, VFB = voltage needed on gate to get E-field = 0 everywhere (flat bands). Note, this can be zero (“ideal” MOS), but generally depends on gate Φm or doping, qVFB =
  2) Threshold voltage, VT = voltage needed on gate to get electron concentration at Si/SiO2 surface same as that of (majority) holes in the bulk. I.e. Φs(inv) = 2ΦF and Si surface is “inverted”.

## Slide 10
In general, voltage applied on the gate will be:
  Where Vi = Eid = voltage dropped across SiO2 insulator
  And Φs = voltage dropped in the Si (surface potential)
Q: what is Vi when V = VFB?
Three interesting regions of MOS operation:
  Accumulation (V < VFB for pMOS)
  Depletion (VFB < V < VT)
  Inversion (VT < V)
Let’s take them one by one:

## Slide 11
Accumulation: V < VFB, holes accumulate at the surface
Vi
|qVi|

## Slide 12
Depletion: VFB < V < VT, holes pushed back in substrate
  Surface is depleted of mobile carriers
  All surface charge is due to fixed dopant atoms
Again, we apply depletion approximation we used for p-n diode: assume abrupt displaced charge (rectangular). Draw:
qVi

## Slide 13
Charge density in depleted region:
Poisson’s equation in depleted region:
Integrate twice (from bulk x = W to surface x = 0 to obtain surface Φs or depletion depth W:
To find Φs as a function of gate V we need all voltage drops.
  Across insulator: Vi = Eid = Qd/Ci where
  Qd is depletion charge in silicon substrate, Qd = -qNAW =
Finally, VG = VFB + Φs + Vi =
We can now solve from the surface potential vs. gate V: