## Slide 1: ECE 340 Lecture 3 Crystals and Lattices
Online reference: http://ece-www.colorado.edu/~bart/book
Crystal Lattices:
  Periodic arrangement of atoms
  Repeated unit cells (solid-state)
  Stuffing atoms into unit cells
  Diamond (Si) and zinc blende (GaAs) crystal structures
  Crystal planes
  Calculating densities

## Slide 2
Appendix III in your book (semiconductors):
Where crystalline semiconductors fit in (electrically):

## Slide 3
The periodic lattice:
Stuffing atoms into unit cells:
  How many atoms per unit cell?
  Avogadro’s number: NA = # atoms / mole
  Atomic mass: A = grams / mole
  Atom counting in unit cell: atoms / cm3
  How do you calculate density?

## Slide 4
The Silicon lattice:
Si atom: 14 electrons occupying lowest 3 energy levels:
  1s, 2s, 2p orbitals filled by 10 electrons
  3s, 3p orbitals filled by 4 electrons
Each Si atom has four neighbors
“Diamond lattice”
How many atoms per unit cell?

## Slide 5
Zinc blende lattice (GaAs, AlAs, InP):
  Two intercalated fcc lattices

## Slide 6
Crystallographic notation

## Slide 7
Crystallographic planes and Si wafers
Si wafers usually cut along {100} plane with a notch or flat side to orient the wafer during fabrication

## Slide 8
Where do (pure) Si wafers come from?
  Read sections 1.3-1.4 in Streetman book
  Take ECE 444
  Short answer:
Image sources: Wikipedia

## Slide 9: ECE 340 Lecture 4 Bonds & Energy Bands

## Slide 10
Graphite (~pencil lead) = parallel sheets of graphene
Carbon nanotube = rolled up sheet of graphene

## Slide 11
The Bohr model of the (isolated) Si atom (N. Bohr, 1913):
Note: inner shell electrons screen outer shell electrons from the positive charge of the nucleus (outer less tightly bound)
Bohr model:

## Slide 12
Quantum theory on two slides:
1) Key result of quantum mechanics (E. Schrödinger, 1926):
  Particle/wave in a single (potential energy) box
  Discrete, separated energy levels

## Slide 13
2) Key result of wave mechanics (F. Bloch, 1928):
  Plane wave in a periodic potential
  Wave momentum k only unique up to 2π/a
  Only certain electron energies allowed, but those can propagate unimpeded (theoretically), as long as lattice spacing is “perfectly” maintained‼!
  But, resistance introduced by: __________ and __________

## Slide 14
Energy levels when atoms are far apart:
Energy levels when atoms are close together (potentials interact):
Energy levels from discrete atoms to crystal lattice:

## Slide 15
Energy states of Si atom expand into energy bands of Si lattice
Lower bands are filled with electrons, higher bands are empty in a semiconductor
The highest filled band = ___________ band
The lowest empty band = ___________ band
Insulators?
Metals?

## Slide 16
Band structure explains why SiO2 (diamond, etc) is insulating, silicon is semiconducting, copper is a metal
For electrons to be accelerated in an electric field they must be able to move into new, unoccupied energy states.
Water bottle flow analogy (empty vs. full)
So, what is a hole then?

## Slide 17
In devices we usually draw:
Simplified version of energy band model, indicating
  Top edge of valence band (EV)
  Bottom edge of conduction band (EC)
  Their separation, i.e. band gap energy (EG)

## Slide 18
Typical semiconductor band gaps (EG) between 0-3 eV
  GaAs → EG ≈ 1.42 eV
  Si → EG ≈ 1.12 eV
  Ge → EG ≈ 0.67 eV
… for more, see Appendix III in book
Insulator band gaps > 5 eV  SiO2 EG = 9 eV
Where are all electrons at T=0 K?
Do either insulators or semiconductors conduct at 0 K?
What about at T=300 K?
ECE 340 Lecture 5 Energy Bands, Temperature, Effective Mass

## Slide 19
mechanical
analogy:
bond picture:
(here 2-D)
band
picture:

## Slide 20
How do band gaps vary with lattice size? (is there a trend?)
How do band gaps
vary with temperature?

## Slide 21
Short recap, so we are comfortable switching between:
  Bond picture
  Band picture vs. x
  Band picture vs. k

## Slide 22
Let’s combine energy bands vs. k and vs. x:
Note what is potential, kinetic, and total energy
Note which way energy of holes increases

## Slide 23
Electrons (or holes) as moving particles:
Newton’s law still applies: F = m*a
Where m* = the “effective mass” of the particle,
which includes all the complex influences of the
crystal potential on the motion of the electron (or hole).
Acceleration?
  For electrons: For holes:
Effective mass values? Fractions of m0. See Appendix III.
  Sometimes depend on direction of motion in the crystal.
  E.g. for electrons in Si: ml = 0.98m0, mt = 0.19m0
  Can also depend on particle location in the band (bottom, top, edge, “light” band vs. “heavy” band).
  Values in Appendix III are given at the bottom of C-band for electrons, top of V-band for holes.

## Slide 24
Q: What is the meaning of the energy band slope in the E-x band diagram picture?