## Slide 1: ECE 340 Lecture 9 Temperature Dependence of Carrier Concentrations
L7 and L8: how to get electron & hole concentrations at:
  Any temperature
  Any doping level
  Any energy level
Previously we also derived:
Where
And

## Slide 2
So the intrinsic carrier concentration at any T is:
What does this tell us?
Note that mn*=1.1m0 and mp*=0.56m0
These are ________________________ effective masses in Si, not to be confused with _______________________
Does the band gap EG change with T?

## Slide 3
Plot log10 of ni vs. T
What do we expect?
Note your book plots this vs. 1000/T in Fig. 3-17; why?
What is this (simple) plot neglecting?

## Slide 4
Recall ni is very temperature-sensitive! Ex: in Silicon:
  While T = 300  330 K (10% increase)
  ni = ~1010  ~1011 cm-3 (10x increase)
Also note:
  Now we can calculate the equilibrium electron (n0) and hole (p0) concentrations at any temperature
  Now we can calculate the Fermi level (EF) position at any temperature
Ex: Calculate and show position of Fermi level in doped Ge (1016 cm-3 n-type) at -15 oC, using previous plot

## Slide 5
Assume Si sample doped with ND = 1015 cm-3 (n-type)
How does n change with T? (your book plots this vs. 1000/T in Fig. 3-18)
Recall the band diagram, including the donor level.
Note three distinct regions:
  Low, medium, and high-temperature

## Slide 6
So far, we assumed material is either just n- or p-doped and life was simple. At most moderate temperatures:
  n0 ≈
  p0 ≈
What if a piece of Si contains BOTH dopant types? This is called compensation.
Group V elements are _______
and introduce ________
Group III elements are _______
and introduce ________

## Slide 7
Case I, assume we dope with ND > NA
  Additional electrons and holes will _____________ until you have n0 ≈ ND - NA and p0 ≈ _________
Case II, what if we introduce ND = NA dopants?
  The material once again becomes ____________ and n0 ≈ p0 ≈ ______
Case III and more generally, we must have charge neutrality in the material, i.e. positive charge = negative charge, so p0 + ND = __________

## Slide 8
So most generally, what are the carrier concentrations in thermal equilibrium, if we have both donor and acceptor doping?
And how do these simplify if we have ND >> NA (n-type doping dominates)?
When is “>>” approximation OK?

## Slide 9: ECE 340 Lectures 10-11 Carrier drift, Mobility, Resistance
Let’s recap 5-6 major concepts so far:
Memorize a few things, but recognize many.
  Why? Semiconductors require lots of approximations!
Why all the fuss about the abstract concept of EF?
  Consider (for example) joining an n-doped piece of Si with a p-doped piece of Ge. How does the band diagram look?

## Slide 10
So far, we’ve learned effects of temperature and doping on carrier concentrations
But no electric field = not useful = boring materials
The secret life of C-band electrons (or V-band holes): they are essentially free to move around, how?
Instantaneous velocity given by thermal energy:
Scattering time (with what?) is of the order ~ 0.1 ps
So average distance (mean free path) travelled between scattering events L ~ _______

## Slide 11
But with no electric field (E=0) total distance travelled is: ___
So turn ON an electric field:
F = ± qE
F = m*a  a =
Between collisions, carriers accelerate along E field:
  vn(t) = ant = ______________ for electrons
  vp(t) = apt = ______________ for holes
Recall how to draw this in the energy band picture

## Slide 12
On average, velocity
is randomized again
every τC (collision time)
So average velocity in E-field is: v = _____________
We call the proportionality constant the carrier mobility
This is a very important result!!! (what are the units?)
What are the roles of mn,p and τC?

## Slide 13
Then for electrons: vn = -μnE
And for holes: vp = μpE
Mobility is a measure of ease of carrier drift in E-field
  If m↓ “lighter” particle means μ…
  If τC↑ means longer time between collisions, so μ…
Mobilities of some undoped (intrinsic) semiconductors at room temperature:

## Slide 14
What does mobility (through τC) depend on?
  Lattice scattering (host lattice, e.g. Si or Ge vibrations)
  Ionized impurity (dopant atom) scattering
  Electron-electron or electron-hole scattering
  Interface scattering
Which ones depend on temperature?
Qualitative, how?
Strongest scattering, i.e. lowest mobility dominates.

## Slide 15
Qualitatively
Quantitatively we rely on experimental measurements (calculations are difficult and not usually accurate):
http://www.ioffe.rssi.ru/SVA/NSM/Semicond/Si/electric.html

## Slide 16
Once again, qualitatively we expect the mobility to decrease with total impurities (ND+NA)
Why total impurities and not just ND or NA? (for electrons and holes?)

## Slide 17
In linear scale, from the ECE 340 course web site:

## Slide 18
Ex: What is the hole drift velocity at room temperature in silicon, in a field E = 1000 V/cm? What is the average time and distance between collisions?

## Slide 19
Now we can calculate current flow in realistic devices!
Net velocity of charge particles  electric current
Drift current density ∝ net carrier drift velocity
∝ carrier concentration
∝ carrier charge
First “=“ sign always applies. Second “=“ applies typically at low-fields (<104 V/cm in Si)
(charge crossing plane of area A in time t)

## Slide 20
Check units and signs:
Total drift current:
Has the form of Ohm’s Law!
Current density:
Current:
This is very neat. We derived Ohm’s Law from basic considerations (electrons, holes) in a semiconductor.

## Slide 21
Resistivity of a semiconductor:
What about when n >> p? (n-type doped sample)
What about when n << p? (p-type doped sample)
Drift and resistance:

## Slide 22
Experimentally, for Si at room T:
This is absolutely essential to show our control over resistivity via doping!
Notes:
  This plot does not apply to compensated material (with comparable amounts of both n- and p-type doping)
  This plot applies most accurately at low-field (<104 V/cm)